## Slide 1
Automated Chemical Vulnerability Assessment of Canvas Paintings from XRF Spectral Imaging Using Deep Learning and Foundation Models
Dimitrije Pešić · Janko Vukobratović · Aleksandra Stojanović · Giulia Ristori · Stefano Ridolfi · Maja Gajić-Kvaščev · Goran Kvaščev
University of Belgrade, School of Electrical Engineering · Ars Mensurae Rome · IDArtScience Rome · Vinča Institute of Nuclear Sciences
7,200
XRF spectra
< 70 s
end-to-end
r > 0.98
reproducibility
0 labels
training data
Science Conference 2026

## Slide 2
Motivation
Why automate conservation risk assessment?
THE PROBLEM
• Historical paintings degrade silently — damage often invisible until irreversible
• Pigments interact chemically: Cu greens corrode, Pb whites turn black, Fe catalyzes oxidation
• Traditional assessment: expert-driven, qualitative, does not scale to full surfaces
XRF MACRO-SCANNING
• Per-pixel elemental maps across entire painting surface
• 120 × 60 = 7,200 spectra at 3 s/pixel
• Non-invasive, no sampling required
• Problem: interpreting 7,200 spectra manually is impractical
OUR ANSWER
• Fully automated pipeline
• Raw XRF → conservation-priority map
• Zero expert-labeled training data
• Under 70 s on a standard laptop
Key principle: preserve as much original material as possible → detect risk before it is visible

## Slide 3
Pipeline Overview
Five stages · no labeled training data · <70 s end-to-end
1
Self-Supervised Denoising
1D U-Net Poisson splitting
→
2
Elemental Extraction
5-pt calibration ROI + background sub.
→
3
NMF Corroboration
K=5 components <5% recon. error
→
4
Chemical Vulnerability Index
5 literature rules Geometric mean
→
5
SAM Region Segmentation
13 regions Per-region CVI
INPUT: raw .mca spectra
OUTPUT: per-region risk report
U-Net inference
28 s · 40%
Extraction + NMF
10.5 s · 15%
CVI + metrics
3.5 s · 5%
SAM segmentation
28 s · 40%

## Slide 4
Spectral Analysis
Denoising → calibration → element maps → NMF corroboration
SELF-SUPERVISED DENOISING
• XRF counts follow Poisson statistics
• Noise2Self: Binomial-split spectrum into two halves (x, y)
• Train 1D U-Net to predict y from x → no clean reference needed
• 4-level encoder/decoder, ~1.66M params, PNLL loss
ELEMENTAL EXTRACTION
• 5-point linear calibration: E = 0.0292·c − 0.069 keV (R² > 0.9999)
• ROI integration + linear background from off-peak sidebands
• Spectral overlap corrections (Cu Kβ→Zn, Pb/As regression)
• As/Pb Lα overlap at ΔE = 0.007 keV — below detector FWHM
NMF (K=5) independently recovers the same 5 material groups — Pb, Ca/Fe, Cu, Ti, Compton — reconstruction error <5% → cross-validates physics-based extraction

## Slide 5
Chemical Vulnerability Index (CVI)
Literature-grounded degradation risk, pixel-level
CVI(i,j) = max_k { w_k · √( A_k(i,j) · B_k(i,j) ) }
• Geometric mean → high score only when BOTH incompatible elements co-occur
• Single-element rules (R2, R3): CVI_k = w_k · A_k
• All intensities percentile-normalised → CVI in [0, 1]
• Gaussian filter σ=1 px to suppress pixel-level noise
FOUR RISK ZONES
Low <0.25
No action
Moderate 0.25–0.50
Monitor
Elevated 0.50–0.75
Intervene
Critical ≥0.75
Urgent
DEGRADATION RULES
ID
Mechanism
Elem.
w
R1
TiO₂/CaCO₃ thermal mismatch
Ti / Ca
0.40
R2
Cu-based green pigment degradation
Cu
1.00
R3
Lead white darkening (PbS)
Pb
1.00
R4
Trapped moisture under TiO₂
Ti / Cu
0.60
R5
Fe-catalyzed Pb oxidation
Fe / Pb
0.80
Sensitivity: ±15% weight perturbation → <8% change in mean CVI · top-decile ranking preserved in >92% of pixels

## Slide 6
Results
Reproducibility · CVI distribution · SAM region analysis
SCAN REPRODUCIBILITY
Two scans, 7 days apart, same conditions
Ca Kα
0.992
Fe Kα
0.993
Pb Lα
0.991
Cu Kα
0.983
Ti Kα
0.982
Composite CVI (prova1 vs prova2)
W₁=0.0054
r=0.994
SSIM=0.982
Without denoising: W₁ +65%, SSIM −0.018 → U-Net improves stability but physics-based extraction is dominant source of agreement
CVI ZONE DISTRIBUTION
Low
13.9%
Moderate
49.9%
Elevated
30.3%
Critical
5.9%
R2 (Cu degradation) elevated on ~22% of pixels R3 (Pb darkening) on ~19% R5 traces figural contours
SAM REGION ANALYSIS
13 regions auto-identified
Pb-dominated
max CVI 0.93 · mean 0.54
Urgent (R3 – Pb darkening)
Cu-dominated
max CVI 0.97 · mean 0.45
Monitor (R2 – Cu degr.)
Ti/Cu overlap
mean CVI ≈ 0.45
Moisture entrapment (R4)

## Slide 7
Further Work & Conclusions
Limitations and next steps
WHAT WE SHOWED
• Fully automated XRF → conservation-priority map in <70 s
• No expert-labeled training data at any stage
• Cross-scan reproducibility r > 0.98 on all elements
• Composite CVI stable across scans (W₁ = 0.0054, SSIM = 0.982)
• 13 SAM regions with per-region risk summaries
• CVI critical zone: 5.9% of pixels flagged
PRINCIPAL LIMITATION
All validation is internal consistency on one mockup canvas — ground-truth comparison against conservator assessments on real paintings with documented degradation outcomes is required.
NEXT STEPS
Validate CVI against expert conservator assessments on real paintings with known degradation outcomes
Integrate NMF abundance maps as CVI inputs — capture material mixtures invisible to single-element thresholds
Extend to paintings with different conservation histories; adapt rule weights as needed
Resolve As/Pb Lα overlap (ΔE=0.007 keV) with higher-resolution detectors or deconvolution
Build conservator-facing GUI/API — no Python expertise required
The contribution is the workflow itself: end-to-end automation of a procedure that traditionally requires extensive expert analysis.